|  |  |
| --- | --- |
| Specific weight (wet product ) | ~ 2000 Kg/m³ |
| Compression strength  | >20 MPa |
| Flexural strength  | >4 MPa |
| Footfall improvement | ΔLw = 13 dB |
| Footfall imporvement on resilient | ΔLw = up to 35 dB |
| Thermal conductivity (λ) | 1,40 WmK |
| Water for mixture  | ~ 15% |
| Recommendedt thickness | >50 mm |
| Operating temperature  | +5°C + 30°C |
| Processing time  | ~ 40 minutes |
| Performance (weight for cm of thickness) | ~ 20 Kg |
| Drying  | As common screed  |